## Slide 1: Material Characterization of Thermoplastic Polyurethanes for 3D Printing
Zoey Mikalatos
Mentors: Kelly Hollenbeck, Conor Harris, Dr. Skip Rochefort

## Slide 2: Introduction
3D Printing
Thermoplastic Polyurethane (TPU)
  Soft polymer
  Not commonly printed
  Different types
    95A and 75D

## Slide 3
SHORE HARDNESS AND DUROMETER
https://www.smooth-on.com/pw/site/assets/files/30090/durometerchart.png

## Slide 4: Background - Printer
Fused Deposition Modeling (FDM)
3 extruders
https://s3-eu-west-1.amazonaws.com/3dhubs-knowledgebase/intro-fdm-3d-printing/3-fdm-schematic.png

## Slide 5: Overview
  Purpose
  Characterization of 95A and 75D TPU for printing
  Establish connection between thermal characterization of polymer and print quality at different print temperatures
  Method
  Differential Scanning Calorimeter (DSC)
  Melt Flow Index (MFI)
  Line printing on the 3D printer

## Slide 6: Applications
Capable of 3D printing parts which need to be flexible
  Parts for the lab
Adhesion between different polymers
Characterizing new polymers for 3D printing

## Slide 7
Differential Scanning Calorimetry (DSC)
Controls
Sample
Flange
Two passes
10-15mg of polymer
-80°C to 280°C (95A)
-80°C to 250°C (75D)

## Slide 10
3ntr 3D Printer
Printed strips 1mm by 250mm
Starting at 240°C, moving down in increments of 2°C until polymer does not flow or adhere any longer
Time the printer as it prints the strips (105 seconds)
Find the mass of the strips
Mass over time gives mass flow rate
Look at quality of strips
Notes: FDM printing – fused deposition modeling

## Slide 13
Piston
Heated Barrel
Controls
Die
Melt Flow Index
Verification that the polymer flows
18°C above the DSC melt temperature
1.1kg weight on piston
240 seconds melt time
3 cuts, 20 seconds between cuts
3 trials for each polymer, 5g per trial
95A TPU at 230°C
  MFI = 39.0 g/10 min
75D TPU at 220°C
  MFI = 19.8 g/10 min

## Slide 14: Conclusions
DSC, MFI, and line printing tests
Printing parameters for different hardness TPUs
  95A: Good print quality from 210°C to 220°C, best flow rate at 220°C
  75D: Good print quality from 212°C to 230°C, best flow rate at 228°C

## Slide 15: Future Work
Differences in adhesion in different types of TPU
  95A adhesion compared to 75D adhesion
Correlation of characterization and printing quality for different polymers

## Slide 16: Acknowledgements
Dr. Skip Rochefort
Kelly Hollenbeck
Conor Harris
Sylvia Sorenson
Oregon State University
Saturday Academy

## Slide 17
Questions?